## Slide 1: Probabilistic Fracture Simulation of Materials
Submitted to
Prof Rajib Chowdhary
Submitted by
Abhinandan Sharma
Enrollment number
20523001
Civil Engineering Department, IIT Roorkee

## Slide 2: Introduction
This seminar topic focuses on :
The Fundamentals of the fracture mechanics
computational methodology on furthering the understanding of fundamental fracture phenomena.
The methodology for probabilistic fracture mechanics analysis (PFM)
based on the crack tip stress and strain fields and the non-linear fracture mechanics have been developed. Their applications to the studies of fracture initiation and stable crack growth may differ because of the difference in the basic postulates of various fracture theories.
The current numerical approaches to the solution of fracture mechanics problems.

## Slide 3: Fundamental Basis Of Fracture Mechanics
For Fracture initiation for brittle materials ∂Uε/∂a ≥ ∂Us/∂a, Uε and US are strain energy and surface energy; and a, crack length.
K characterizes crack tip stresses, strains and displacements forms the fundamental basis of the linear elastic fracture mechanics rather than the global energy balance.
Recently crack tip stress, strain and displacement fields can be characterized by J, which is a contour independent integral or rate of potential energy change during the cracking process in a non-linear elastic solid. J has been widely used to study non-linear fracture mechanics.
At the fracture initiation of a cracked brittle solid in the condition of fixed grip, the release rate of the stored strain energy equals or exceeds the dissipative surface energy rate.
γ, the surface energy per unit area;

## Slide 4: Defining Fracture
The “crack” suddenly starts to propagate internally at A.
The increased crack length increases the compliance of the specimen and causes the sudden load drop from A to A’.
As the load increases, the crack continues its internal growth.
At B, the crack front at the specimen surface starts to move forward, and the crack continues to grow in a “stable”manner to the maximum load C.
D is the point of final separation,
fracture mechanics studies the fracture initiation at A and the stable crack growth from A’ to B and onwards.
Often the point of fracture initiation is not so clearly defined as shown in the figure. In this case, certain degree of arbitrariness has to be introduced in order to define fracture initiation. Fracture can be defined in terms of the above described macrofeatures or in terms of the micro-structural features such as fracture of brittle inclusions, etc

## Slide 5: Griffith Criterion
Griffith proposed the criterion of brittle fracture based on the principle of global energy balance.
where U ε is the strain energy and U γ is the surface energy.
which is constant. For a small crack in a large plate, we have, at fracture.
.
γ, the surface energy per unit area;
Uγ is surface energy; Uε is strain energy; and Up is plastic work

## Slide 6: Global Energy Balance Theory
At fracture we have:
It is known that Uγ ≪ Up . Neglect Uγ , we get:
The relation between work dissipation U p and crack lengh ”2a” can be found. The classic plasticity theory shows, rp ∝ a , and Up ∝ rp2 which gives
Uγ is surface energy; Uε is strain energy; and Up is plastic work.
rp= plastic zone

## Slide 7: Global Energy Balance Theory
But there can be vast differences in the experimental and the theoritical data
In order to explain the observed experimental phenomena, it is necessary to resort to the difference in the state of crack tip stress field. The lower plastic energy dissipation rate in the state of plane strain is caused by the triaxial state of tensile stress, which causes reductions in effective stress, plastic deformation, and plastic energy dissipation; and it causes an increase in maximum tensile stress and an earlier fracture initiation.
The experimental evidences that demonstrate the failure of the global energy balance are well known. But they have not been recognized as such. Figure shows the thickness effects on fracture toughness. The fracture toughness varies from 40 MPa√m for KIc , to the maximum value of 107 MPa√m. The strain energy release rates of the two limiting cases of plane strain and plane stress states differ by a factor of (1 − ν2 ).v is Poisson’s ratio. The difference is approximately 10%. If the plastic energy dissipation rate is constant, the difference in fracture toughnesses should not be more than 10%.

## Slide 8: Sharp Notch Analysis
All crack tips are “blunted,” so sharp notches and cracks can be considered as equivalents.
The fracture stress of a notched specimen depends on notch root radius, R.
We will consider sharp elleptical notches in large plates under tensile loading in a direction perpendicular to the major axis.When a solid contains a sharp notch of initial root radius Ri , the radius increases with the applied load. If the root radius increment, ∆R is much larger than Ri , the fracture stress σc is independent of Ri . If the size of the fracture process zone, ρF is much larger than Ri , σc will also be independent of Ri . In our analysis, we assume R is always less than Rc

## Slide 9: Fracture Process Zone
Materials are inhomogeneous
They contain brittle and ductile phases, inclusion particles, grain boundaries, etc. Fracture initiation in a cracked solid is often in the interior of a specimen, where the high tensile stress exists at the locations of brittle and weak materials.
Once a local fracture is initiated, it spreads out.
They contain brittle and ductile phases, inclusion particles, grain boundaries, etc. Fracture initiation in a cracked solid is often in the interior of a specimen, where the high tensile stress exists at the locations of brittle and weak materials.
The fracture at inclusion I increases the stress at inclusion 2, and the increased stress causes the fracture of inclusion 2. Ductile fracture takes place between the brittle particles. If the brittle inclusions are large and closely spaced, it may cause an avalanche effect, one particle fracturing rapidly after the other. The fracturing process stops when the crack is out of the zone of the high tensile stress in the plane strain triaxial state of tension. The crack extension could be sizable and could cause noticeable load drop. This is the well known phenomenon of pop-in and is a local instability. Hence, Klc is the result of a local instability phenomenon, not a global instability.

## Slide 10: Fracture Toughness And Fracture Ductility
The initiated local fracture will continue to propagate. The extent of fracture propagation varies according to the “brittleness” of the material. The fracturing processes can be classified in three categories.
(1) Once initiated, the localized fracture will continue to grow rapidly across the specimen without further increase in σ∞ or K. It is very brittle .
(2) Once initiated, the localized fracture will continue to grow to a sizable extent in a rapid manner while σ∞ and K drop. After the initial fracture, it needs to increase K in order to continue to grow further. Fracture is initiated in the interior in the plane strain region, and the initial fracturing process will stop when the crack is out of the zone of triaxial state of tension.
(3) If fracture initiation is caused by brittle particles and if the brittle particles are small and far apart, once the local fracture is initiated, it needs a considerable amount of plastic deformation to grow across the regions

## Slide 11: Numerical Methods For Solution Of Fracture Problems
Finite difference method is the oldest technique for the solution of boundary value problems. The method directly involves the solution of the governing differential system in an approximate manner by subdividing the domain of interest into a connected series of discrete points called nodes. These nodes are the sampling points for the solution and are linked using the finite difference operators to the governing equations.
Integral equation methods basic approach employed involves an analytic formulation of the elasticity problem to the point of a singular integral equation. The singularity is then extracted and the result is a non-singular integral equation which can be solved quite accurately with any number of techniques.
Employment of the finite difference operators results in a system of algebraic equations for the discrete nodal values of the field variable. The finite difference method can be used to discretize both space and time. The finite difference method is difficult to use for irregularly shaped domains or for problems involving singularities, because the fine meshing required near a singularity cannot easily be reduced for the rest of the domain
This approach yields excellent solutions; however, it requires an extensive analytic formulation which is different for each new problem. The method is quite useful, nonetheless, for establishing benchmark solutions to compare with other methods as the degree of accuracy can be guaranteed. The method is only applicable to elasticity problems (without non-linearities). For three-dimensional problems, the derivation of the integral equations becomes quite laborious.

## Slide 12: Numerical Methods For Solution Of Fracture Problems
Boundary Integral Equation Method (BIEM) is a numerical approach to the solution of linear boundary value problems with known Green’s function solutions. The boundary of the domain of interest is discretized using ”elements” which are interconnected at discrete points called nodes.
Finite Element Method is the most widely employed numerical method for fracture mechanics problems. The formulation of the FEM is based on a variational statement of the governing physics. For the problems of linear elasticity, the Principle of Virtual Work, given by

## Slide 13: Numerical Methods For Solution Of Fracture Problems

## Slide 14: Probabilistic Fracture Mechanics
The problem is divided in:
1. The basic problem: The two main considerations are the distribution of (1)crack-like defects introduced during the fabrication of a structure and (2)the critical crack length distribution for the material under service conditions. From a failure point of view, it is importanl to know how this distribution compares with that of the critical crack size, which is controlled by the material properties, and applied loading. The probability of failure is then given by the probability of interaction of the actual crack or flaw ai , and a critical crack length ac.
2. Further considerations: Closely linked with the as fabricated flaw size distribution is the role played by non-destructive testing in detecting defects which may, or may not, be repaired.
In situations where fatigue cracking occurs, the defect distribution will tend to alter with the number of applied cycles.
Many factors contribute to reliability and these often change both systematically and at random. In the past, structures have been designed using a simple factor of safety approach to calculate a safe lifetime over which the applied loads will be sustained. Each variable in the equations governing the operation of the system was given a reasonable value drawn from past results or even just human intuition, and a predicted life obtained. This was then divided by a factor of safety which reduced it to give a ’safe’ maximum operating life. It was conceivable that this is unrealistically conservative but simple.
One approach is to use historical data from past failures and non-failures to evaluate the reliability of current productions.
An alternative approach has been sought, namely the development and application of engineering models based on an understanding of the failure modes and statistical distributions of the controlling parameters.Ideally, a combination of the two methods is necessary so that past experience and results plus specially designed laboratory tests can be used to obtain statistical distributions which best fit these data, but also, hopefully provide predictions about altered or new systems.
the latter being controlled primarily by the fracture toughness.
,In general, there is a lack of data for the initial distribution of defects in a structure so the distribution is often assumed to be lognormal or exponential
This problem may be reduced by in-service inspection at fixed intervals of time, and by repairing the defects so found.

## Slide 15: Statistical Basis Of PFM
The basis of PFM is the simple axiom that a given mode of failure event E will occur when the stress σw associated with the failure mode exceeds the mode governing strength σf . The probability of failure mode E is given by
In the probabilistic treatment, the random variations are described using distributions of values for the parameters rather than one deterministic value. The distribution may be thought of as a curve combining the possible values and the likelihood (probability) they will occur. The introduction of distributions of values necessarily complicates an analysis, but the end result is likely to be more accurate and hence of more use. In some cases, neat analytical expressions for the reliability are impossible and numerical approximations are required. Approximate interactive algebraic procedures are used to determine an estimate of the failure probability ( = 1 - reliability), whereas in the latter, the approximation is at a later stage, after all the exact probabilistic expressions have been obtained for the complete system; this ibe justified by the improvement gained.s, of course, much harder, and the work involved may not be justified by the improvement gained.
with i = 1.....nx , depends on input variables that at affect component stress or strength or both. An alternative definition in terms of a strength ratio Y = σf /σw is equally valid and leads to P(E)=P((Y )< 1)

## Slide 16: Statistical Basis Of PFM
Here, G is a concise deterministic summary of all prior engineering experience, models, and assumptions. If the engineering analysis does not lead to an obvious functional form, G may be obtained from standard least- squares fitting of the engineering data or by the repetitive analysis procedure.the xi are most realistically described as random variables Xi rather than single assigned deterministic values. Statistical interpretation of the Xi results in the interpretation of strength margin as a random variable. The statistical interpretation also allows the analyst to quantify his uncertainty of the engineering model G based on judgement, and his previous record of predictive success and failure. This error quantification is done by introducing one or more additional Xi to serve as ’error terms’. The cumulative distribution functions of the Xi , represented b

## Slide 17: PFM by using Monte Carlo simulation and Scaled Boundary Finite Element Method
For Monte Carlo simulation (MCS) method , uncertainties in the applied load, material properties, and crack geometry are modeled as random variables described by specific probability distribution functions.
The scaled boundary finite-element method is employed to investigate the shape sensitivity of the stress intensity factors of a crack to the size and orientation of the crack. Only a single boundary mesh is required. The variation of the crack size and orientation can be represented by simply changing the position of the crack tip without the need for remeshing the boundary.
Therefore, the repetitive deterministic analysis is made simple, elegant, and highly efficient as compared to most other numerical methods. Thus, it becomes feasible to use the brute force MCS method for the reliability analysis of a cracked structure.
For each of the Monte Carlo samples, the SIFs, which are sensitive to the randomness of the variables, are computed. The resulting SIFs are compared with the material toughness to evaluate whether failure will occur.

## Slide 18: Scaled Boundary Finite Element Method
The geometry of the domain satisfies the scaling requirement, i.e., the whole boundary of the domain is directly visible from the crack tip.
Problems of more complex geometry can be divided into such smaller subdomains. The scaling center O is selected at the crack tip.
Without loss of generality, the origin of the Cartesian coordinates x̂ and ŷ is defined at the scaling center.
The boundary is discretized with line elements. The nodal coordinates at the boundary are denoted {x} and {y}, with shape functions [N (η)] in the local coordinate η . Thus for any point on the boundary the Cartesian coordinates (x, y), can be interpolated by

## Slide 19: Scaled Boundary Finite Element Method
The coordinates of any point within the domain (x̂, ŷ) can then expressed as:
where the scaling factor ξ takes the value of 0 at the scaling center and 1 on the boundary.
ξ and η are called the scaled boundary coordinates.
To avoid the Jacobian of the scaled boundary coordinate transformation approaching zero, the acute angle formed by a radial line and the boundary should not be too small.

## Slide 20: Scaled Boundary Finite Element Method
As shown in Figure below for a single 2-node element, nodal displacement functions u(ξ) are introduced along the radial lines passing through the scaling center O and a node on the boundary. Along the circumferential direction η , the displacements is obtained by interpolating the nodal displacement functions
Applying a weighted residual technique in the η direction leads to the following scaled boundary finite element equation in displacement
The global coefficient matrices [E0], [E1]and [E2]
are obtained by assembling the element coefficient
matrices same manner as for the stiffness matrices
where [D] is the elasticity matrix. where [B1(η)] and [B2(η)] describe the strain-displacementt

## Slide 21: Scaled Boundary Finite Element Method
The displacement functions u(ξ) are expressed as
where [Si ](i = 1, 2, ..., N ) are diagonal blocks of the real Schur matrix, [Ψi(u) ] the corresponding displacement modes and c integration constants, which are determined from the displacements on the boundary u(ξ = 1)

## Slide 22: Scaled Boundary Finite Element Method
Evaluation of stress intensity factors:
When the real parts of the eigenvalues of a diagonal block [Si] are between -1 and 0, the matrix power function leads to a stress singularity. The diagonal block is denoted as [S(s) ] (superscript (s) for singular) and −1 < λ[S(s)] < 0 applies. The corresponding displacement modes and integrationconstants are denoted as [Ψ(s)] and {C(s)}Their contribution to stresses vanishes when the limit ξ→0 is performed and thus are not needed for the definition of stress intensity factors. The singular stress field is expressed as

## Slide 23: Scaled Boundary Finite Element Method
Mode-I failure: During fracture, the material can be associated with its own characteristic resistance to fracture known as the ’fracture toughness’ KIc such that the crack will grow under Mode-I loading when
Mixed-Mode Failure: The failure criteria can be simplified, for 2D Mixed-Mode loading, as

## Slide 24: Scaled Boundary Finite Element Method
Shape sensitivity:

## Slide 25: Monte-Carlo Simulation
The deterministic fracture mechanics problem:
Assume a high toughness material with crack growth relation given by
Range of Stress Intesity is given by
From this we get number of cycles as,
Now we compact and take the logrithmic equation
where C, n are empirically determined constants, a is the radius of a circular crack in the fracture plane, ∆K is the range of stress intensity factor, and Npr is the number of fatigue cycles.
For the case of a buried circular crack remote from the surface and extending through the uniform tensile stress field, we have
where ∆σ is the range of stress If these equations are combined and integrated, the following expression for fatigue life Npr is obtained:
We now consider a buried elliptical crack of fracture plane area Ai = πcb where c ≤ b are the major and minor semi-axes of the elliptical projection of the flaw on the fracture plane. The results of a more advanced analysis, shows that eq. is reasonably accurate for the elliptical crack, with b/c≪40, as well as the circular crack of equal area for which eq. is derived. For the purpose of the PFM analysis below, we compact the notation and take the logarithm of eq. to obtain

## Slide 26: Monte-Carlo Simulation
Distributions of the input random variables C, ∆σ, Ai :
The relationship is obtained from Cr-Mo -V steel crack growth data and is used to compute median crack growth rates in in./cyc. For this steel the mean yield stress is σ̄ = 85ksi. The above assumptions can be compacted into the notation
The probabilistic stress distribution shown is formulated from three assumptions. These are
(1) log-normality;
(2) 95% of the spindle material, by volume, will encounter ∆σ < 0.80σ̄ y;
(3) 95% of the material volume will encounter ∆σ > .25σ̄ y. Finally we assume the flaw size
distribution that is used to determine Ai obeys the relation log Ai = N (−0.9586, 0.750).
that is, log C is a normal random variable with median and mean μc = log(6.76X10 −11 ) and standard deviation Sc . For the example, we further assume a log-normal stress variation of log ∆σ=N̄ (1.5799, 0.1535), which means that Ao has a median value of 38 ksi with 0.1535 standard deviation on log σa due to stress gradients, and spindle-to-spindle design and usage variations.

## Slide 27: Monte-Carlo Simulation
The probabilistic analysis: We assume that each rotor spindle must endure the equivalent of 3000 cycles in service, where each cycle comprises a cold start-up, operation and shut- down. The assumption of constant usage allows a simple definition of Y such as
S standard deviations

## Slide 28: Monte-Carlo Simulation
Probabilistic addition of crack initiation cycles:
The MC program can be utilized to investigate the effect of non-zero initiation life Ni on total fatigue life. For example, the total fatigue life can be written as
where Ni is proportional to D

## Slide 29: Monte-Carlo Simulation

## Slide 30: Monte-Carlo Simulation
Distributions of the input random variables C, ∆σ, Ai :
The relationship is obtained from Cr-Mo -V steel crack growth data and is used to compute median crack growth rates in in./cyc. For this steel the mean yield stress is σ̄ = 85ksi. The above assumptions can be compacted into the notation
The probabilistic stress distribution shown is formulated from three assumptions. These are
(1) log-normality;
(2) 95% of the spindle material, by volume, will encounter ∆σ < 0.80σ̄ y;
(3) 95% of the material volume will encounter ∆σ > .25σ̄ y. Finally we assume the flaw size
distribution that is used to determine Ai obeys the relation log Ai = N (−0.9586, 0.750).
that is, log C is a normal random variable with median and mean μc = log(6.76X10 −11 ) and standard deviation Sc . For the example, we further assume a log-normal stress variation of log ∆σ=N̄ (1.5799, 0.1535), which means that Ao has a median value of 38 ksi with 0.1535 standard deviation on log σa due to stress gradients, and spindle-to-spindle design and usage variations.

## Slide 31
Thank You